## Slide 1: Two Sides of a Coin
Employing
Graphene
To Probe
MEH-PPV
Employing
MEH-PPV
To Probe
Graphene

## Slide 2: Republic of China: Taiwan

## Slide 3: Yuan Ze University EE

## Slide 4: Two Sides of a Coin
Use Graphene
to probe
MEH-PPV
Use
MEH-PPV
to probe
Graphene

## Slide 5: What is Graphene?
C in a 2D hexagonal lattice
big aromatic molecule
Conductor (Q + J)
Graphene oxide

## Slide 6: What is MEH-PPV?
Le MEH-PPV —poly[2-méthoxy-5-(2-éthyl-hexyloxy)-1,4-phénylène-vinylène] — est un polymère semiconducteur de type p (donneur d'électrons)
1D chain folding into a 3D structure w/1D substructure

## Slide 7: Solution: Graphene
observation

## Slide 8: Confocal Microscope Setup

## Slide 9: Two Sides of a Coin
Use Graphene
to probe
MEH-PPV
Use
MEH-PPV
to probe
Graphene

## Slide 10: Tails: Outline
Background and Motivation: MEH-PPV
  What are we trying to understand?
  Why is it important?
  Why do we want to use graphene?
  Terminology
Exciton Model
Results: with and without graphene
Conclusions on Energy migration

## Slide 11: Why MEH-PPV?
Most studied luminescent conjugated polymer
  >1000 papers published in the year 2017 alone
  Research started in 1970s!
Potential Applications: Solar Cells & PLEDs
  Quantum yield in solution 65%
  Drops to 3% in film. Why?
Numerous Single Molecule (SM) studies…
  from 2000 (Nature), one of first molecules studied
  to 2017 (ACS Nanoletters) and beyond
 Prototypical luminescent conjugated polymer
 But still holding secrets…

## Slide 12: Review MEH-PPV Photo-Physics
Photophysics
Roleplay
Ref: https://www.youtube.com/watch?v=T4lyZ5rPbes

## Slide 13: Exciton Model of MEH-PPV (@20)
Longer Conjugation
More Red

## Slide 14: A Picture & A Question
We thought (2000): intra-chain energy is fast
We now know:
  Inter-chain energy transfer fast (<30 ps)
  Intra-chain energy transfer is slow
  Fluorescence lifetime ~ 1 ns
How slow is intra-chain energy transfer?

## Slide 15: Use Quenching to Investigate
Open a new non-radiative channel
To quench the chromophores
Observe lifetime and spectral changes
 approximate rate of intrachain energy transfer

## Slide 16: So our goal is…
Understand changes to MEH-PPV photophysics brought on by quenching of fluorescence due to a nearby external quencher
Use this information to understand the rate of intrachain (kintra) energy transfer.
Note: Quenching vs. Photo-bleaching
  -Both reduce fluorescence
  -Photo-Bleach: permanent (due to chemical changes to fluorophore)
  -Quenching: proximity (disappears when/if quencher is removed)

## Slide 17: Challenge & Solution
Challenge: Energy Transfer between molecules
  Scales with (R/Ro)-6
  Operational length scale: (2 – 8 nm)
  But our molecules are ϕ>10nm
  Complete quench of MEH-PPV not possible
  Difficult data interpretation
Solution: 2D Energy Transfer to 2D material
  Scales with (R/Ro)-4
  Operational length scale: (2 – 30 nm)
  Whole molecule can be quenched.

## Slide 18: Why use Graphene to Quench?
2D material (graphene) vs metal quencher
  Eliminate coupling to surface plasmon polaritons
  Minimize variations in local electric field strength
  More efficient quenching

## Slide 19: MEH-PPV only

## Slide 20: MEH-PPV Spectra (no Quencher)
Extended Chains Dominate

## Slide 21: Photo-Bleaching (no quencher)
Longer
Conjugated
Segments
Bleach First

## Slide 22: Exciton Model of Bleaching

## Slide 23: With Graphene Quench

## Slide 24: MEH-PPV Spectra

## Slide 25: Lifetime/Intensity Quench
99% of emission is quenched
Mean Lifetime drops by 70%

## Slide 26: Photo-Bleaching with Quench
Time Scale: Order of Magnitude Longer
Spectrum: Initially more Blue, Constant

## Slide 27: Exciton Model of MEH-PPV
Constant Spectra  Intrachain energy transfer arrested
 kgraphene > kintra (Note kr~1 ns-1)
Lifetime analysis suggests: kgraphene ~ 4 ns-1
Bounds on the rate of intrachain energy transfer
i.e. 4 ns-1 > kintra > 1 ns-1
Ho X, Nanotechnology 30, 065702 (2019)

## Slide 28: Two Sides of a Coin
Use Graphene
to probe
MEH-PPV
Use
MEH-PPV
to probe
Graphene

## Slide 29: Graphene vs Graphene Oxide (GO)
PL quench has been used to visualize GO/r-GO
Graphene Oxide…
  Quenches almost 100% <5 nm
  Has contrast for dye layers up to 300nm thick
r-GO quenches more efficiently than GO
From Kim J,
JACS 132,
261 (2010)

## Slide 30: What is LAO Graphene?
Graphene in which areas have been selectively oxidized using a voltage difference across an AFM tip
# of sp3 bonds ↓
Between G and GO
How will degree of oxidation affect PL?
Can PL be used to estimate bond reduction?

## Slide 31: Why use MEH-PPV to probe?
State of graphene will affect PL of nearby molecules
Small fluorophore also subject to interface effects  ambiguity
MEH-PPV close to interface PL same as bulk.
Remove interface effects
No graphene
Ho X, Chem Phys Lett 686, 212 (2017)
No graphene

## Slide 32: LAO ↑  Quench ↓

## Slide 33: LAO ↑  Lifetime ↑

## Slide 34: LAO ↑  Survival Time ↓

## Slide 35: Conclusions
Quenching spectroscopy can be used to gain insight into complicated polymer photophysics
Graphene (2D) is an ideal quencher due to its 2D nature (extended quench range) and the ability to control distance between the molecule and the quencher (spin coating)
Fluorescence of long chain polymers stable at interfaces
Changes in the fluorescence of long chain polymers can be used to gain insight into the degree of graphene oxidation/reduction.
GO ↑ 
  PL intensity ↑,
  Spectrum ,
  lifetime ↑
  survival time ↑,

## Slide 36: Welcome to Taiwan / Welcome to YZU

## Slide 37: Welcome to Taiwan / Welcome to YZU

## Slide 38: Welcome to Taiwan / Welcome to YZU
↑
TBCA: https://youtu.be/iGDBLIYcFS8?t=132

## Slide 39: An Invitation
Title: Surviving Breast Cancer – The Role of Faith
Date: Sunday August 18, 2019
Time: 11:30 am
Venue: Park Royal Bible Church, 2400 Truscott Drive, Mississauga, ON L5J 2B2
Language: Chinese (Mandarin) & English
↑